| BNG Metals | Product specification PS‑Fe01 · Rev A · 10.2026 |
| --- | --- |

| Iron oxide pigment Red synthetic pigment · concrete and coatings | Fe 26 |
| --- | --- |

Fe₂O₃

Target specification   Colour (L*a*b*), tinting strength and oil absorption to be set by December 2027 laboratory work. Fallback: iron ore concentrate, shipped bulk.

| Parameter | Unit | Specification | Method |
| --- | --- | --- | --- |
| Iron oxide, Fe₂O₃ | % w/w | min 95.0 | ISO 1248 |
| Colour difference vs. reference, ΔE* | — | to be set | ISO 787‑1 / 7724 |
| Relative tinting strength | % | to be set | ISO 787‑24 |
| Oil absorption | g/100 g | 20 – 30 | ISO 787‑5 |
| Water-soluble matter | % w/w | max 0.5 | ISO 787‑3 |
| Sieve residue, 45 µm | % w/w | max 0.1 | ISO 787‑7 |
| Moisture | % w/w | max 1.0 | ISO 787‑2 |
| pH, aqueous suspension | — | 4.0 – 8.0 | ISO 787‑9 |

| Origin and route Kalyumnoye deposit, Republic of Buryatia. Primary rock (synnyrite), alkaline separation. | Packaging 25 kg valve bags on 1,000 kg pallets · 1,000 kg FIBC. Store dry. |
| --- | --- |
| Registration EN 12878 (pigments for cement-based materials) — planned. REACH — planned. EAEU — in progress. | Technical contact BNG Elements, Metals desk · metals@bng-elements.com · +7 ··· |

| © BNG Elements 2026 · This sheet supersedes PS‑Fe01 Rev — | Page 1 of 2 · EN · RU on reverse |
| --- | --- |

| БНГ Металс | Спецификация продукта PS‑Fe01 · Ред. A · 10.2026 |
| --- | --- |

| Пигмент оксида железа Красный синтетический пигмент · бетон и лакокрасочные материалы | Fe 26 |
| --- | --- |

Fe₂O₃

Целевая спецификация   Цвет (L*a*b*), красящая способность и маслоёмкость устанавливаются по лабораторным работам декабря 2027 года. Запасной вариант — железорудный концентрат, навалом.

| Показатель | Ед. изм. | Норма | Метод |
| --- | --- | --- | --- |
| Оксид железа, Fe₂O₃ | % масс. | не менее 95,0 | ISO 1248 |
| Цветовое отличие от эталона, ΔE* | — | устанавливается | ISO 787‑1 / 7724 |
| Относительная красящая способность | % | устанавливается | ISO 787‑24 |
| Маслоёмкость | г/100 г | 20 – 30 | ISO 787‑5 |
| Водорастворимые вещества | % масс. | не более 0,5 | ISO 787‑3 |
| Остаток на сите 45 мкм | % масс. | не более 0,1 | ISO 787‑7 |
| Влажность | % масс. | не более 1,0 | ISO 787‑2 |
| pH, водная суспензия | — | 4,0 – 8,0 | ISO 787‑9 |

| Происхождение и передел Месторождение Калюмное, Республика Бурятия. Первичная порода (сыннырит), щелочное разделение. | Упаковка Клапанные мешки 25 кг на поддонах 1 000 кг · биг-бэги 1 000 кг. Хранить в сухом месте. |
| --- | --- |
| Регистрация EN 12878 (пигменты для цементных материалов) — запланировано. REACH — запланирован. ЕАЭС — в процессе. | Технические контакты БНГ Элементс, отдел Металс · metals@bng-elements.com · +7 ··· |

| © БНГ Элементс, 2026 · Настоящая спецификация заменяет PS‑Fe01 Ред. — | Страница 2 из 2 · RU · EN на лицевой стороне |
| --- | --- |