| BNG Agro | Product specification PS‑K04.B · Rev A · 10.2026 |
| --- | --- |

| Potassium silicate Solid potassium silicate · granular grade | K 19 |
| --- | --- |

K₂SiO₃

Target specification   Values are design targets based on the chosen technological production process in 2026. Confirmation by pilot results, summer 2028.

| Parameter | Unit | Specification | Method |
| --- | --- | --- | --- |
| Silica, SiO₂ | % w/w | min 66.0 | Gravimetric |
| Potassium oxide, K₂O | % w/w | min 32.0 | GOST 20851.3 |
| Molar ratio SiO₂ : K₂O | — | 2.0 – 2.2 | Calculated |
| Moisture | % w/w | max 2.0 | GOST 20851.4 |
| Water insoluble | % w/w | max 0.5 | Gravimetric |
| Iron, Fe | % w/w | max 0.05 | ICP‑OES |
| Particle size | SGN | 40 – 50 | Fertilizer industry standard |
| pH, 1% solution | — | min 11.0 | Potentiometric |

| Origin and route Kalyumnoye deposit, Republic of Buryatia. Primary rock (synnyrite), alkaline separation. | Packaging 25 kg PE-lined bags on 1,200 kg pallets · 1,000 kg FIBC with liner. Store dry — hygroscopic. |
| --- | --- |
| Registration EAEU / GOST — in progress. EU FPR conformity — planned. Country files on request. | Technical contact BNG Elements, Agro desk · agro@bng-elements.com · +7 495 114 50 50 |

| © BNG Elements 2026 · This sheet supersedes PS‑K04.B Rev A —09.2026 | Page 1 of 2 · EN · RU on reverse |
| --- | --- |

| БНГ Агро | Спецификация продукта PS‑K04.B · Ред. A · 10.2026 |
| --- | --- |

| Силикат калия Твёрдый силикат калия · гранулированная марка | K 19 |
| --- | --- |

K₂SiO₃

Целевая спецификация   Значения — проектные цели утвержденной производственной технологии в 2026 году. Подтверждение по результатам опытной установки, лето 2028 года.

| Показатель | Ед. изм. | Норма | Метод |
| --- | --- | --- | --- |
| Кремнезём, SiO₂ | % масс. | не менее 66,0 | Гравиметрический |
| Оксид калия, K₂O | % масс. | не менее 32,0 | ГОСТ 20851.3 |
| Мольное отношение SiO₂ : K₂O | — | 2,0 – 2,2 | Расчётный |
| Влажность | % масс. | не более 2,0 | ГОСТ 20851.4 |
| Нерастворимый в воде остаток | % масс. | не более 0,5 | Гравиметрический |
| Железо, Fe | % масс. | не более 0,05 | ICP‑OES |
| Гранулометрический состав | SGN | 40 – 50 | Стандарт индустрии удобрений |
| pH, 1% раствор | — | не менее 11,0 | Потенциометрический |

| Происхождение и передел Месторождение Калюмное, Республика Бурятия. Первичная порода (сыннырит), щелочное разделение. | Упаковка Мешки 25 кг с ПЭ-вкладышем на поддонах 1 200 кг · биг-бэги 1 000 кг с вкладышем. Хранить в сухом месте — гигроскопичен. |
| --- | --- |
| Регистрация ЕАЭС / ГОСТ — в процессе. Соответствие Регламенту ЕС по удобрениям — запланировано. Страновые досье по запросу. | Технические контакты БНГ Элементс, отдел Агро · agro@bng-elements.com · +7 495 114 50 50 |

| © БНГ Элементс, 2026 · Настоящая спецификация заменяет PS‑K04.B Ред.A —09.2026 | Страница 2 из 2 · RU · EN на лицевой стороне |
| --- | --- |